## Slide 1: Constitutive modelling in arterial mechanics
Alessandro Giudici
Maastricht University, The Netherlands
12 February 2026, Auckland

## Slide 2
Table of content:
Introduction
Thick- vs. thin-wall modelling
Experimental considerations
Viscoelasticity
Constitutive modelling in vivo

## Slide 3
Constitutive equations: Strain energy density function
“Constitutive equation [...] is a relation between two or more physical quantities that is specific to a material […] and approximates its response to external stimuli”.
Wikipedia
Strain energy density function
[Pa] = [J/m3]
Right Cauchy-Green tensor
Deformation gradient tensor
principal directions
shear
Orthotropic deformation

## Slide 4
Constitutive equations: Linking energy to measurable quantities
Strain energy density function
[Pa] = [J/m3]
Right Cauchy-Green tensor
Deformation gradient tensor
Cauchy stress tensor
[Pa]
Lagrange multiplier

## Slide 5
Equilibrium equations
Radial equilibrium equation:
Axial equilibrium equation:
0

## Slide 6
Equilibrium equations: Radial equilibrium
0
Laplace’s law
Thin wall

## Slide 7
Equilibrium equations: Axial equilibrium
Thin wall

## Slide 8
What constitutive equations to use? – Pressure
Pressure
Diameter
elastin
collagen
vascular smooth muscle cells (VSMCs)
matrix
(elastin)
collagen
VSMCs
Arterial wall tissue model
Chow, Biophysical J 2014; 106(12): 2684-92.
Fonck, Am J Physiol J 2007; 292(6): H2754-63.
Schriefl, Acta Biomater 2015; 17: 125-36.
Quick, Am J Physiol Heart Circ Physiol, 1996, 271(6): H2669-76.

## Slide 9
Isobaric transducer force–length relationships
Force [103 dynes]
Length [cm]
Aorta
Femoral artery
Carotid artery
Length [cm]
Length [cm]
Force [103 dynes]
Force [103 dynes]
van Loon, Biorehology 1977; 14(4): 181-201
in vivo
axial length
What constitutive equations to use? – Transducer force

## Slide 10
What constitutive equations to use? – In vivo axial stretch
carotid

## Slide 11
Parametrisation
aorta
Circ. stress [MPa]
Axial stress [MPa]
Axial stretch [-]
Circ. stretch [-]
Axial stretch [-]
Circ. stretch [-]

## Slide 12
Table of content:
Introduction
Thick- vs. thin-wall modelling
Experimental considerations
Viscoelasticity
Constitutive modelling in vivo

## Slide 13
Thick- vs Thin-walled modelling
Thin-wall modelling assumptions:
  wall thickness radius:
  uniform stresses:

## Slide 14
Tri-layered arterial wall structure

## Slide 15
Tri-layered arterial wall structure
Ascending aorta
Intima
Descending thoracic aorta
Intima
Media
Adventitia
Media
Adventitia
Giudici, J Biomech Behav Biomed Mater 2023; 141: 105752
aorta
Ascending aorta
Descending thoracic aorta
Wall
Wall

## Slide 16
Unless assumptions are made on some parameters based on microscopy or literature data:
  Wang et al. 2016, J Biomech, 49:2358-2365
  Polzer et al. 2015, Acta Biomater, 14:133-145
  Fata et al. 2014, J Biomech Eng, 136(2): 021009
Tri-layered constitutive model
High number of unknown parameters
Layers
Assembly
Model parameters
Overfitting
Intima constitutive model
Media constitutive model
Adventitia constitutive model
Hybrid solution: Tri-layered thin-walled model
Giudici, Ann Biomed Eng 2021, 49:2454-2467.
Tri-layered constitutive model
A multi-scale computational model which simultaneously recapitulates:
Major constituents within each arterial layer
The three arterial layers individually
The whole-organ mechanics of the artery

## Slide 17
Giudici, Ann Biomed Eng 2021, 49:2454-2467.
Hybrid solution: Tri-layered thin-walled model
aorta
Intimal matrix
Intimal collagen
Medial matrix
Medial collagen
Adventitial matrix
Adventitia collagen

## Slide 18
Giudici, J Mech Behav Biomed Mater 2023, 141:105752.
Functional uniqueness of the ascending aorta
aorta
Relative change in stored elastic energy over a 40 mmHg pressurisation [%]