## Slide 1
Table of content:
Introduction
Thick- vs. thin-wall modelling
Experimental considerations
Viscoelasticity
Constitutive modelling in vivo

## Slide 2
Planar biaxial testing: Experimental flexibility
?
=
Stretched
Compressed
Deformation field?

## Slide 3
Giudici, Artery Res 2022, 28: 41:54.
Planar vs. physiological biaxial testing
aorta

## Slide 4
Planar vs. physiological biaxial testing
Circumferential stretch
1
2
2
1.5
Axial stretch
1.5
Planar biaxial testing
L = 95%
L = 100%
L = 105%
Inflation testing
Extension testing
Cindy van Loo
carotid

## Slide 5
Planar vs. physiological biaxial testing
Cindy van Loo
carotid
Constitutive model 1
Constitutive model 2
Simulation
(tube2planar)
Simulation
(planar2tube)

## Slide 6
Planar vs. physiological biaxial testing
Cindy van Loo
carotid
Four-fibre model to capture both datasets
(8 parameters).
Two-fibre model to capture the planar biaxial data
(4 parameters).

## Slide 7
Table of content:
Introduction
Thick- vs. thin-wall modelling
Experimental considerations
Viscoelasticity
Constitutive modelling in vivo

## Slide 8
Viscoelasticity: Experimental observations
The loading rate affects the arterial response.
aorta
Myrthe van der Bruggen

## Slide 9
Viscoelasticity: Experimental observations
The loading rate affects the arterial response.
The stiffening effect is modulated by pressure.
aorta

## Slide 10
Stress
Strain
Deformation independent viscoelastic behaviour
Deformation dependent viscoelastic behaviour?
Constituent-based quasi-linear viscoelasticity
Matrix elastic model
Collagen elastic model
Elastic arterial model
Matrix viscoelastic
model
Collagen viscoelastic model
Giudici, Biomech Mod Mechanobiol 2023, 22:1607-1623.
Viscoelastic arterial model

## Slide 11
Viscoelastic collagen-dominated behaviour
=
Large stiffening
Elastic matrix-dominated behaviour
=
Small stiffening
carotid
Giudici, Biomech Mod Mechanobiol 2023, 22:1607-1623.
Constituent-based quasi-linear viscoelasticity

## Slide 12
aorta
van der Laan,… Giudici, J Biomech 2024, 171:112190.
Examples: Freezing
Koen van der Laan

## Slide 13
aorta
van der Laan, Neutel, …, Giudici. AJP – Cell 2025, 329(5):C1398-410.
Examples: Ageing (in mice)
Koen van der Laan
Cédric Neutel

## Slide 14
aorta
Pencheva, …, Giudici,… Cardiovasc Diabetol 2025, 329(5):C1398-410.
Examples: Diabetes and advanced glycation end products
Margarita Pencheva

## Slide 15
Table of content:
Introduction
Thick- vs. thin-wall modelling
Experimental considerations
Viscoelasticity
Constitutive modelling in vivo

## Slide 16
Sparse in vivo biomechanical data

## Slide 17
Pressure [mmHg]
Thickness-to-diameter ratio [-]
Y = young
O = old
Learoyd. Circ Res 1966, 18(3):278-92.
Sommer, AJP Heart Circ Physiol 2009; 298:H898-912.
van der Laan, AJP Cell 2025, 329(5):C1398-410.
Giudici, J Mech Behav Biomed Mater 2023, 141:105752.
Giudici, PhD Thesis 2021.
How to deal with the axial behaviour?
Constant pressure–force relationship.
Vascular homeostasis.
Pressure
Transducer force
Inner diameter
Pressure

## Slide 18
Sparse in vivo biomechanical data
elastin
collagen
VSMCs

## Slide 19
elastin
collagen
VSMCs
elastin
collagen
VSMCs
elastin
collagen
VSMCs
elastin
collagen
VSMCs
Sparse in vivo biomechanical data
Time

## Slide 20
In vivo biomechanics: How to deal with limited data?
60-day head down bead rest (HDBR) study:
  Measurements at the carotid, femoral, and popliteal artery.
  Tonometer pressure and ultrasound diameter and IMT.
Baseline
HDBR
Day 29
HDBR
Day 52
Recovery
Day 12
Recovery
Day 30
Boutouyrie, J Hypertens 2022, 40: 2058–2067.
Carotid artery
Femoral artery
Popliteal artery

## Slide 21
We are hiring!

## Slide 22: QUESTIONS?
Biomedical Engineering
Bart Spronck
Koen Reesink
Tammo Delhaas
Cédric Neutel
Mobina Izadpanah
Myrthe van der Bruggen
Koen van der Laan
Cindy van Loo
Internal Medicine
Margarita Pencheva
Casper Schalkwijk
Paris Cardiovascular
Research Centre
Pierre Boutouyrie
Rosa Maria Bruno
Biochemistry
Leon Schurgers
Durham University
Ashraf Khir
Cambridge University
Ian Wilkinson
University of Amsterdam
Shaiv Parikh
Yale University
Jay Humphrey
Carnegie Mellon University
Jason Szafron
Iowa State University
Abhay Ramachandra
a.giudici@maastrichtuniversity.nl